Stainless steel 304 material analysis report

| Name |  | Stainless steel plate |  |  |  | Style |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No |  | 3WJ391 |  |  |  | piece |  | 1 |  |
| Company |  | Jiangsu Zhengheng Light Industrial Machinery Co,ltd |  |  |  | State |  | Drilling |  |
| No |  |  |  |  |  | Sample date |  | Feb 27th,2016 |  |
| Analysis gist |  |  |  |  |  | Report date |  | Feb 27th,2016 |  |
| Analysis element |  | Pls see below form |  |  |  |  |  |  |  |
| No | Element mark | Standard value % | Measured value % | No | Element mark |  | Standard value % |  | Measured value % |
| 1 | C | / | 0.044 | 6 | Cr |  | / |  | 18.00 |
| 2 | Si | / | 0.559 | 7 | Ni |  | / |  | 8.15 |
| 3 | Mn | / | 1.09 | 8 | Mo |  | / |  | / |
| 4 | P | / | 0.023 | 9 | Ti |  | / |  | -- |
| 5 | S | / | 0.002 | 10 | V |  | / |  | / |
|  |  | / | / | 11 | Cu |  | / |  | / |
| Conclusion | Analysis this sample and offer above factural measured report |  |  |  |  |  |  |  |  |